## Slide 1: Introduction to Nondestructive Testing
Notes: This presentation was developed by the Collaboration for NDT Education to provide students and other audiences with a general introduction to nondestructive testing. The material by itself is not intended to train individuals to perform NDT functions, but rather to acquaint individuals with some of the common NDT methods and their uses. All rights are reserved by the authors but the material may be freely used by individuals and organizations for educational purposes. The materials may not be sold commercially, or used in commercial products or services.
This presentation is one of nine developed by the Collaboration for NDT Education. The topics covered by the other presentations are:
Visual Inspection
Penetrant Testing
Magnetic Particle Testing
Eddy Current Testing
Ultrasonic Testing
Radiographic Testing
Welder Certification
Weld inspection with UT
Public educators can request a free copy of the presentations by contacting the Collaboration at NDT-ed@cnde.iastate.edu.
Comments are welcome at NDT-ed@cnde.iastate.edu.

## Slide 2: Outline
Introduction to NDT
Overview of Six Most Common NDT Methods
Selected Applications

## Slide 3: Definition of NDT
The use of noninvasive
techniques to determine
the integrity of a material,
component or structure
or
quantitatively measure
some characteristic of
an object.
i.e. Inspect or measure without doing harm.

## Slide 4: Methods of NDT
Visual
Liquid Penetrant
Magnetic Particle
Eddy Current
Ultrasonic
X-ray
Microwave
Acoustic Emission
Thermography
Laser Interferometry
Replication
Flux Leakage
Acoustic Microscopy
Magnetic Measurements
Tap Testing

## Slide 5: What are Some Uses of NDE Methods?
Flaw Detection and Evaluation
Leak Detection
Location Determination
Dimensional Measurements
Structure and Microstructure Characterization
Estimation of Mechanical and Physical Properties
Stress (Strain) and Dynamic Response Measurements
Material Sorting and Chemical Composition Determination
Fluorescent penetrant indication

## Slide 6: When are NDE Methods Used?
  To assist in product development
  To screen or sort incoming materials
  To monitor, improve or control manufacturing processes
  To verify proper processing such as heat treating
  To verify proper assembly
  To inspect for in-service damage
There are NDE application at almost any stage
in the production or life cycle of a component.

## Slide 7: Six Most Common NDT Methods
Visual
Liquid Penetrant
Magnetic
Ultrasonic
Eddy Current
X-ray

## Slide 8: Visual Inspection
Most basic and common inspection method.
Tools include fiberscopes, borescopes, magnifying glasses and mirrors.
Robotic crawlers permit observation in hazardous or tight areas, such as air ducts, reactors, pipelines.
Portable video inspection unit with zoom allows inspection of large tanks and vessels, railroad tank cars, sewer lines.

## Slide 9: Liquid Penetrant Inspection
A liquid with high surface wetting characteristics is applied to the surface of the part and allowed time to seep into surface breaking defects.
The excess liquid is removed from the surface of the part.
A developer (powder) is applied to pull the trapped penetrant out the defect and spread it on the surface where it can be seen.
Visual inspection is the final step in the process. The penetrant used is often loaded with a fluorescent dye and the inspection is done under UV light to increase test sensitivity.

## Slide 10: Magnetic Particle Inspection
The part is magnetized. Finely milled iron particles coated with a dye pigment are then applied to the specimen. These particles are attracted to magnetic flux leakage fields and will cluster to form an indication directly over the discontinuity. This indication can be visually detected under proper lighting conditions.

## Slide 11: Magnetic Particle Crack Indications

## Slide 12: Radiography
The radiation used in radiography testing is a higher energy (shorter wavelength) version of the electromagnetic waves that we see as visible light. The radiation can come from an X-ray generator or a radioactive source.
High Electrical Potential
Electrons
-
+
X-ray Generator or Radioactive Source Creates Radiation
Exposure Recording Device
Radiation
Penetrate
the Sample

## Slide 13: Film Radiography
Top view of developed film
X-ray film
The part is placed between the radiation source and a piece of film. The part will stop some of the radiation. Thicker and more dense area will stop more of the radiation.
= more exposure
= less exposure
The film darkness (density) will vary with the amount of radiation reaching the film through the test object.

## Slide 14: Radiographic Images

## Slide 15: Eddy Current Testing
Conductive
material
Coil
Coil's
magnetic field
Eddy
currents
Eddy current's
magnetic field

## Slide 16: Eddy Current Testing
Eddy current testing is particularly well suited for detecting surface cracks but can also be used to make electrical conductivity and coating thickness measurements. Here a small surface probe is scanned over the part surface in an attempt to detect a crack.

## Slide 17: Ultrasonic Inspection (Pulse-Echo)
High frequency sound waves are introduced into a material and they are reflected back from surfaces or flaws.
Reflected sound energy is displayed versus time, and inspector can visualize a cross section of the specimen showing the depth of features that reflect sound.
f
plate
crack
0
2
4
6
8
10
initial
pulse
crack
echo
back surface
echo
Oscilloscope, or flaw detector screen

## Slide 18: Ultrasonic Imaging
Gray scale image produced using the sound reflected from the front surface of the coin
Gray scale image produced using the sound reflected from the back surface of the coin (inspected from “heads” side)
High resolution images can be produced by plotting signal strength or time-of-flight using a computer-controlled scanning system.

## Slide 19: Common Application of NDT
Inspection of Raw Products
Inspection Following Secondary Processing
In-Services Damage Inspection

## Slide 20: Inspection of Raw Products
Forgings,
Castings,
Extrusions,
etc.

## Slide 21: Inspection Following Secondary Processing
Machining
Welding
Grinding
Heat treating
Plating
etc.

## Slide 22: Inspection For In-Service Damage
Cracking
Corrosion
Erosion/Wear
Heat Damage
etc.

## Slide 23: Power Plant Inspection
Probe
Signals produced by various amounts of corrosion thinning.
Periodically, power plants are shutdown for inspection.
Inspectors feed eddy current probes into heat exchanger tubes to check for corrosion damage.
Pipe with damage

## Slide 24: Wire Rope Inspection
Electromagnetic devices and visual inspections are used to find broken wires and other damage to the wire rope that is used in chairlifts, cranes and other lifting devices.

## Slide 25: Storage Tank Inspection
Robotic crawlers use ultrasound to inspect the walls of large above ground tanks for signs of thinning due to corrosion.
Cameras on long articulating arms are used to inspect underground storage tanks for damage.

## Slide 26: Aircraft Inspection
Nondestructive testing is used extensively during the manufacturing of aircraft.
NDT is also used to find cracks and corrosion damage during operation of the aircraft.
A fatigue crack that started at the site of a lightning strike is shown below.

## Slide 27: Jet Engine Inspection
Aircraft engines are overhauled after being in service for a period of time.
They are completely disassembled, cleaned, inspected and then reassembled.
Fluorescent penetrant inspection is used to check many of the parts for cracking.

## Slide 28: Crash of United Flight 232
Sioux City, Iowa, July 19, 1989
A defect that went undetected in an engine disk was responsible for the crash of United Flight 232.

## Slide 29: Pressure Vessel Inspection
The failure of a pressure vessel can result in the rapid release of a large amount of energy. To protect against this dangerous event, the tanks are inspected using radiography and ultrasonic testing.

## Slide 30: Rail Inspection
Special cars are used to inspect thousands of miles of rail to find cracks that could lead to a derailment.
Notes: The heavy loads that trains place on the railroad tracks can result in the formation of cracks in the rail. If these cracks are not detected, they can lead to a derailment. Special rail cars equipped with NDT equipment are used to detect rail defects before they are big enough to cause serious problems.

## Slide 31: Bridge Inspection
The US has 578,000 highway bridges.
Corrosion, cracking and other damage can all affect a bridge’s performance.
The collapse of the Silver Bridge in 1967 resulted in loss of 47 lives.
Bridges get a visual inspection about every 2 years.
Some bridges are fitted with acoustic emission sensors that “listen” for sounds of cracks growing.
Notes: The US has 578,000 highway bridges, which are the lifelines of US commerce. Corrosion, cracking and other damage can all affect the bridges load carrying capacity. Therefore, all of the elements that directly affect performance of the bridge including the footing, substructure, deck, and superstructure must be periodically inspected or monitored. Visual inspection is the primary NDE method used to evaluate the condition of the majority of the nation's highway bridges. Inspectors periodically (about every two years) pay each bridge a visit to assess its condition. However, it is not uncommon for a fisherman, canoeist and other passerby to alert officials to major damage that may have occurred between inspections.
The potential penalties for ineffective inspection of bridges can be very severe. Instances of major bridge collapse are very rare, but the results are truly catastrophic. The collapse of the famous Silver Bridge at Point Pleasant, Ohio in 1967 resulted in loss of 47 lives. The cost of this disaster was 175 million dollars but some experts estimate the same occurrence today would cost between 2.1 and 5.6 billion dollars. Furthermore, these cost figures do not take into account factors such as loss of business resulting from loss of access or detours, the cost resulting from blockage of a major river shipping channel, and potential environmental damage due to hazardous materials being transported over the bridge at the time of collapse.
Fatigue cracking and corrosion will become increasingly important considerations as we go beyond the 75 year life expectancy and current visual inspection techniques will not suffice. The life extension approach will require increased use of NDE in a coordinated effort to obtain reliability assurance for these structures. NDE techniques such as magnetic particle inspection and ultrasonic inspection are being used with greater frequency. One of the newer NDE technologies being used is acoustic emission (AE) monitoring. Some bridges are being fitted with AE instruments that listen to the sounds that a bridge makes. These sophisticated systems can detect the sound energy produced when a crack grows and alert the inspector to the cracks presence. Sensors can be permanently fixed to the bridge and the data transmitted back to the lab so that continuous bridge condition monitoring is possible. The image provided here shows field engineers installing an AE monitoring system on the lift cables of the Ben Franklin Bridge in Philadelphia, PA

## Slide 32: Pipeline Inspection
NDT is used to inspect pipelines to prevent leaks that could damage the environment. Visual inspection, radiography and electromagnetic testing are some of the NDT methods used.
Remote visual inspection using a robotic crawler.
Radiography of weld joints.
Magnetic flux leakage inspection. This device, known as a pig, is placed in the pipeline and collects data on the condition of the pipe as it is pushed along by whatever is being transported.

## Slide 33: Special Measurements
Boeing employees in Philadelphia were given the privilege of evaluating the Liberty Bell for damage using NDT techniques. Eddy current methods were used to measure the electrical conductivity of the Bell's bronze casing at a various points to evaluate its uniformity.

## Slide 34: For More Information on NDT
The Collaboration for NDT Education
www.ndt-ed.org
The American Society for Nondestructive Testing
www.asnt.org