## Slide 1
Flaw Scattering Models

## Slide 2
Learning Objectives
Far-field scattering amplitude
Kirchhoff approximation
Born approximation
Separation of Variables
Examples of scattering of simple shapes
(spherical pore, flat crack, side-drilled hole)

## Slide 3
Flaw Scattering
rs
es
xs
y
n
flaw
ei
p0
Incident plane
wave
p0 … pressure
amplitude
Fluid Model
At many wavelengths away from the flaw the
scattered waves are spherical waves
scattered pressure
A is called the plane wave far-field scattering amplitude

## Slide 4
plane wave far field scattering amplitude of the flaw
Flaw Scattering
rs
es
xs
y
n
flaw
ei
p0
Incident plane
wave
p0 … pressure
amplitude
Fluid Model

## Slide 5
Flaw Scattering
To obtain the far field scattering amplitude, we need to know the
pressure and velocity on the surface of the flaw due to the incident
and scattered waves
These quantities can be found by solving a flaw scattering
boundary value problem.

## Slide 6
Flaw Scattering
Elastic Solid
rs
n
flaw
U0
U0 … displacement
amplitude for wave
of type  ( = P,S) in
problem (1)
Scattered wave of
type  (= P,S)
scattered displacement
from a flaw
P-wave
S-wave

## Slide 7
Flaw Scattering
Vector scattering amplitude for a scattered wave of
type  due to a plane wave of unit displacement
amplitude and type
elastic
constants
displacements and displacement
gradients

## Slide 8
Flaw Scattering
The received voltage in some measurement models is related to a specific component of the vector scattering amplitude given by
3-D scattering amplitude
polarization vector of an incident wave from receiving transducer (to be discussed shortly)

## Slide 9
Flaw Scattering
A() can be obtained from:
Analytical/Numerical methods
Separation of variables
Boundary Elements (BEM)
Finite Elements (FEM)
Method of Optimal Truncation (MOOT)
T-matrix
Kirchhoff Approximation
Born Approximation
or A() can be found experimentally through
deconvolution:
measure
model, measure

## Slide 10
Flaw Scattering
Kirchhoff Approximation for a Volumetric Flaw
on the "lit" surface: fields are those from plane waves
interacting with a plane surface
on the rest of the surface the fields are assumed to be zero

## Slide 11
Flaw Scattering
It has been recently shown that the pulse-echo scattering amplitude response, A(), for a stress-free flaw (void or crack) in an elastic solid is identical to the scalar (fluid) scattering amplitude:

## Slide 12
Flaw Scattering-Spherical Void
For the pulse-echo response of a spherical
void of radius a
0
5
10
15
20
25
30
0
0.1
0.2
0.3
0.4
0.5
0.6
0.7
frequency, MHz
|A()|
a = 1 mm
c = 5900m/s
2a

## Slide 13
0
5
10
15
20
25
30
0
0.2
0.4
0.6
0.8
1
1.2
1.4
frequency, MHz
2|A|/a
Comparison with Kirchhoff solution with
exact separation of variables solution for the P-P scattering
amplitude of a void in an elastic solid (pulse-echo)
leading edge
response
"creeping" wave
exact solution (solid line)
Kirchhoff solution
(dotted line)
Flaw Scattering-Spherical Void

## Slide 14
Inverting the scattering amplitude (fluid model) into the
time domain
A(t)
t
leading edge
response
"lit" surface
response
Flaw Scattering-Spherical Void

## Slide 15
Exact solution
for a void in an
elastic solid (time
domain)
vs the Kirchhoff
approximation solution
time,

sec
-
2
0
2
4
6
8
10
-
1.5
-
1
-
0.5
0
0.5
1
1.5
2
2.5
time,

sec
-
2
0
2
4
6
8
10
-
1.5
-
1
-
0.5
0
0.5
1
1.5
2
2.5
creeping wave
Flaw Scattering-Spherical Void

## Slide 16
Although the Kirchhoff approximation is formally a high frequency approximation ( ka >>1), numerical tests have shown it capable of producing good agreement (<1 dB difference) for the peak-to-peak time domain response of the spherical void down to ka =1 provided the bandwidth is sufficient
bandwidth, %
ka
10
20
30
40
50
60
70
80
90
0.5
1
1.5
2
2.5
3
3.5
4
4.5
5
white: differences <1 dB
gray: >1 dB but < 1.5 dB
black: > 1.5 dB
Flaw Scattering-Spherical Void

## Slide 17
Flaw Scattering-Inclusion
Leading Edge Response - General Convex Inclusion
(scattered mode same as incident mode)
High frequency, stationary phase approximation
Plane wave reflection coefficient
Gaussian curvature of flaw surface at
stationary phase point

## Slide 18
Flaw Scattering-Inclusion
In the time domain
Leading Edge Response - General Convex Inclusion
(scattered mode same as incident mode)

## Slide 19
Flaw Scattering-Crack
Kirchhoff Approximation – Flat Elliptical Cracks

## Slide 20
General pitch-catch crack response-circular crack
The magnitude of the P-wave pulse-echo far-field scattering amplitude versus frequency for a 1 mm radius circular crack in steel
with an angle of incidence of from the crack normal.
0
5
10
15
20
25
30
0
0.2
0.4
0.6
0.8
1
1.2
1.4
1.6
1.8
frequency, MHz
0
5
10
15
20
25
30
0
0.2
0.4
0.6
0.8
1
1.2
1.4
1.6
1.8
frequency, MHz
Flaw Scattering-Crack

## Slide 21
Comparison of the Kirchoff approximation and MOOT for a 0.381 mm radius circular crack at an incident angle of 45 degrees (pulse-echo)
0
5
10
15
20
25
0
0.05
0.1
0.15
0.2
0.25
frequency, MHz
amplitude
KIR
MOOT
inc = 45
Flaw Scattering-Crack

## Slide 22
When eq is parallel to the crack normal, n :
Special case - pulse echo:
ei
es
n
eq
ei
es
n
The magnitude of the P-wave pulse-echo far-field scattering amplitude versus frequency for a 1 mm
radius circular crack in steel at normal incidence.
0
5
10
15
20
25
30
0
2
4
6
8
10
12
14
16
frequency, MHz
0
5
10
15
20
25
30
0
2
4
6
8
10
12
14
16
frequency, MHz
Flaw Scattering-Crack

## Slide 23
Comparison of the Kirchoff approximation and MOOT for a 0.381 mm radius crack at normal incidence (pulse-echo)
0
5
10
15
20
25
0
0.2
0.4
0.6
0.8
1
1.2
1.4
1.6
1.8
2
frequency, MHz
amplitude
KIR
MOOT
inc=0
numerical errors in MOOT
Flaw Scattering-Crack

## Slide 24
Inverting these results into the time domain
flash points
Example: pulse-echo
t
Flaw Scattering-Crack

## Slide 25
At normal incidence, for pulse-echo
A
(
e
;
e
)
i
s
t
Flaw Scattering-Crack

## Slide 26
A planar crack is a very “specular” reflector

0
10
20
30
40
50
60
70
80
90
0
0.5
1
1.5
2
2.5
3
angle, degrees
Flaw Scattering-Crack

## Slide 27
white: differences <1 dB
gray: >1 dB but < 1.5 dB
black: > 1.5 dB
Although the Kirchhoff approximation is formally a high frequency approximation ( ka >>1), numerical tests have shown it capable of producing good agreement (<1 dB difference) for the peak-to-peak time domain response of a circular crack at normal incidence down to ka =1.5 provided the bandwidth is sufficient
bandwidth, %
10
20
30
40
50
60
70
80
90
0.5
1
1.5
2
2.5
3
3.5
4
4.5
5
ka
Flaw Scattering-Crack

## Slide 28
Comparison of synthesized waveforms scattered from a 0.381 mm radius crack using the Kirchhoff approximation and MOOT using frequencies from 0-25 MHz approximately (pulse echo)
0
5
10
15
20
25
0
0.1
0.2
0.3
0.4
0.5
0.6
0.7
0.8
0.9
1
amplitude
frequency, MHz
Flaw Scattering-Crack

## Slide 29
0-15 degrees from crack normal
-20
-15
-10
-5
0
5
10
15
20
KIR
MOOT
0
5
10
15
Flaw Scattering-Crack

## Slide 30
20-35 degrees from crack normal
Flaw Scattering-Crack

## Slide 31
40-55 degrees from crack normal
Flaw Scattering-Crack

## Slide 32
60-70 degrees from crack normal
Flaw Scattering-Crack

## Slide 33
75-85 degrees from crack normal
Flaw Scattering-Crack

## Slide 34
Comparison of peak-to-peak values of MOOT and Kirchhoff versus angle of incidence for the 0.381mm radius crack (pulse-echo)
The arrow shows where agreement is within 1 dB
Flaw Scattering-Crack

## Slide 35
Now consider the scattering amplitude with narrow band Gaussian window
The central frequency is 10 MHz, and the bandwidth is 1 MHz
Radius of the crack a = 0.381mm
0
5
10
15
20
25
0
0.1
0.2
0.3
0.4
0.5
0.6
0.7
0.8
0.9
1
frequency, MHz
amplitude
Flaw Scattering-Crack

## Slide 36
the range of angles where the agreement is good is significantly reduced
Flaw Scattering-Crack

## Slide 37
Now consider the scattering amplitude with wider band Gaussian
window
The central frequency is 10 MHz, and the bandwidth is 6 MHz
Radius of the crack a = 0.381mm
0
5
10
15
20
25
0
0.1
0.2
0.3
0.4
0.5
0.6
0.7
0.8
0.9
1
frequency, MHz
amplitude
Flaw Scattering-Crack

## Slide 38
The range of excellent agreement now is back to angles as great as 45 degrees or more
Flaw Scattering-Crack

## Slide 39
Flaw Scattering
10
20
30
40
50
60
70
80
90
10
15
20
25
30
35
40
45
50
55
60
bandwidth, %
max. incident angle, degrees
Maximum incident angle where the peak-to-peak time domain agreement between the Kirchhoff approximation and the exact solution for a circular crack is less than 1 dB for ka =5.0 (other ka values shown same trend).
Flaw Scattering-Crack

## Slide 40
Kirchhoff approximation for pulse-echo scattering of a side-drilled hole (incident direction in plane perpendicular to the hole axis)
L
2b
Bessel function
Struve function
Flaw Scattering-SDH

## Slide 41
Flaw Scattering-SDH
Comparison with exact 2-D separation of variables
solution for P-waves (pulse-echo)
The three-dimensional normalized pulse-echo P-wave scattering amplitude versus normalized wave number for a side drilled hole in the Kirchhoff approximation (solid line) and from the exact two-dimensional separation of variables solution (dashed line).
0
2
4
6
8
10
0
0.1
0.2
0.3
0.4
0.5
0.6
0.7
0.8
0.9
0
2
4
6
8
10
0
0.1
0.2
0.3
0.4
0.5
0.6
0.7
0.8
0.9

## Slide 42
Flaw Scattering-SDH
Comparison with exact 2-D separation of variables
solution for S-waves (pulse-echo_)
The three-dimensional normalized pulse-echo SV-wave scattering amplitude versus normalized wave number for a side drilled hole in the Kirchhoff approximation (solid line) and from the exact two-dimensional separation of variables solution (dashed line).
0
2
4
6
8
10
0
0.2
0.4
0.6
0.8
1
1.1
0
2
4
6
8
10
0
0.2
0.4
0.6
0.8
1
1.1

## Slide 43
Flaw Scattering
Kirchhoff approximation - Summary
For volumetric flaws -the Kirchhoff approximation properly models the leading edge signal as long as ka >1 approximately but does not model other waves (creeping waves, etc.)
For cracks – the Kirchhoff approximation models the flash point signals properly in pulse-echo as long as ka > 1 approximately and the incident angle is less than about 50 degrees for wide band responses. For narrow band responses this angle is considerably reduced to as little as 15-20 degrees.

## Slide 44
Flaw Scattering -Inclusion
The Born approximation assumes that the material of an inclusion differs little from the host material so that to first order the incident wave passes through the inclusion unchanged (weak scattering, low frequency approximation)
incident wave
einc
The Born Approximation

## Slide 45
The Born approximation generally is developed from a volume integral expression for the scattering amplitude
density difference
difference in elastic constants
fields in the flaw replaced by incident fields
Flaw Scattering -Inclusion

## Slide 46
For a spherical inclusion in pulse-echo
spherical Bessel function
where
relative density
difference
relative wave speed
difference
Flaw Scattering -Inclusion

## Slide 47
Corresponding time domain impulse response for a spherical inclusion (pulse-echo)
front surface
response
back surface
response
Flaw Scattering -Inclusion

## Slide 48
Comparison with "exact" separation of variables solution
for the pulse-echo response of a spherical inclusion by synthesizing a time-domain response from frequencies ranging from 0-20 MHz approximately for a 1 mm radius inclusion (10 % differences in properties)
The time domain pulse-echo P-wave response of a 1 mm radius spherical inclusion in steel where the density
and compressional wave speed are both ten percent higher than the host steel. Solid line:
Born approximation, dashed line: separation of variables solution.
-
1
-
0.5
0
0.5
1
-
0.5
0
0.5
1
1.5
amplitude
time,

sec
-
1
-
0.5
0
0.5
1
-
0.5
0
0.5
1
1.5
amplitude
time,

sec
Flaw Scattering -Inclusion

## Slide 49
Comparison with "exact" separation of variables solution
for the pulse-echo response of a spherical inclusion by synthesizing a time-domain response from frequencies ranging from 0-20 MHz approximately for a 1 mm radius inclusion (50 % differences in properties)
The time domain pulse-echo P-wave response of a 1 mm radius spherical inclusion in steel where the density
and compressional wave speed are both fifty percent higher than the host steel.Solid line: Born approximation,
dashed line: separation of variables solution.
amplitude
errors
time of arrival errors
-
1
-
0.5
0
0.5
1
-
4
-
2
0
2
4
6
8
amplitude
time,

sec
-
1
-
0.5
0
0.5
1
-
4
-
2
0
2
4
6
8
amplitude
time,

sec
Flaw Scattering -Inclusion

## Slide 50
Doubly Distorted Born Approximation
replace wave speeds of host material by that of the flaw in the Born approximation
for the pulse-echo response of a spherical
inclusion
where
Flaw Scattering -Inclusion

## Slide 51
The time domain pulse-echo P-wave response of a 1 mm radius spherical inclusion in steel where the density and compressional wave speed are both fifty percent higher than the host steel. Solid line: Doubly Distorted Born approximation, dashed line: separation of variables solution.
Front surface amplitude response is improved, and relative time of arrival of back surface response is correct, but there is an error in absolute time of arrivals (50% differences in properties)
-
1
-
0.5
0
0.5
1
-
4
-
2
0
2
4
6
8
amplitude
time,

sec
-
1
-
0.5
0
0.5
1
-
4
-
2
0
2
4
6
8
amplitude
time,

sec
Flaw Scattering -Inclusion

## Slide 52
Why is the front surface response amplitude improved by the Doubly Distorted Born Approximation ?
Answer: because
(plane wave reflection coefficient)
1
1.2
1.4
1.6
1.8
2
2.2
2.4
2.6
2.8
3
0
0.2
0.4
0.6
0.8
1
1.2
1.4
1.6
1.8
2
1
1.2
1.4
1.6
1.8
2
2.2
2.4
2.6
2.8
3
0
0.2
0.4
0.6
0.8
1
1.2
1.4
1.6
1.8
2
F
R12
Flaw Scattering -Inclusion

## Slide 53
This suggests we apply a phase correction to the doubly distorted Born approximation and replace by
resulting in the modified Born approximation (MBA)
for the pulse-echo response of a spherical
inclusion
phase correction
Flaw Scattering -Inclusion

## Slide 54
The time domain pulse-echo P-wave response of a 1 mm radius spherical inclusion in steel where the density and compressional wave
speed are both fifty percent higher than the host steel.Solid line: MBA approximation, dashed line: separation of variables solution.
The MBA
(50 % differences in properties)
-
1
-
0.5
0
0.5
1
-
2
-
1
0
1
2
3
4
5
6
amplitude
time,

sec
-
1
-
0.5
0
0.5
1
-
2
-
1
0
1
2
3
4
5
6
amplitude
time,

sec
Flaw Scattering -Inclusion

## Slide 55
The time domain pulse-echo P-wave response of a 1 mm radius spherical inclusion in steel where
the density and compressional wave speed are both one hundred percent higher than the host steel.
Solid line: MBA approximation, dashed line: separation of variables solution.
The MBA
(100 % differences in properties)
-
1.5
-
1
-
0.5
0
0.5
1
1.5
2
-
10
-
5
0
5
10
15
20
amplitude
time,

sec
-
1.5
-
1
-
0.5
0
0.5
1
1.5
2
-
10
-
5
0
5
10
15
20
amplitude
time,

sec
Flaw Scattering -Inclusion

## Slide 56
The sphere and the cylinder are the only two geometries
where we can obtain exact separation of variables solutions for elastic wave scattering problems. These are commonly used as "exact" solutions to test more approximate theories and numerical methods.
The Method of Separation of Variables
Flaw Scattering

## Slide 57
Flaw Scattering-Void
Example 1: pulse-echo P-wave scattering of a spherical void

## Slide 58
Flaw Scattering-Void
0
5
10
15
20
25
30
0
0.2
0.4
0.6
0.8
1
1.2
1.4
frequency, MHz
2|A| / b
0
5
10
15
20
25
30
0
0.2
0.4
0.6
0.8
1
1.2
1.4
frequency, MHz
2|A| / b
The normalized P-wave pulse-echo scattering amplitude 2A/b
for a spherical void of radius b.

## Slide 59
Flaw Scattering-Void
Using this separation of variables solutions at many frequencies to synthesize a P-wave impulse time domain solution (pulse-echo)
The time-domain pulse-echo P-wave response of a 0.5 mm radius spherical void in steel ( cp = 5900 m/s, cs = 3200 m/sec)
obtained by applying a low-pass cosine-squared windowing filter between 10 and 20 MHz to the separation
of variables solution and then inverting the result into the time domain with the inverse Fourier transform.
time,

sec
amplitude
-
1
-
0.5
0
0.5
1
1.5
-
12
-
8
-
4
0
6
time,

sec
amplitude
-
1
-
0.5
0
0.5
1
1.5
-
12
-
8
-
4
0
6

## Slide 60
Flaw Scattering-Void
Example 2: pulse-echo SV-wave scattering of a spherical void

## Slide 61
Flaw Scattering-Void
The SV-wave pulse-echo scattering amplitude
The magnitude of the pulse-echo SV-wave response, , versus frequency for a 0.5 mm radius spherical void in steel
( cp = 5900 m/s, cs = 3200 m/sec) as calculated by the method of separation of variables
0
2
4
6
8
10
12
14
16
18
20
0
0.1
0.2
0.3
0.4
0.5
0.6
0.7
frequency, MHz
amplitude
0
2
4
6
8
10
12
14
16
18
20
0
0.1
0.2
0.3
0.4
0.5
0.6
0.7
frequency, MHz
amplitude

## Slide 62
Flaw Scattering-Void
Using this separation of variables solutions at many frequencies to synthesize an SV-wave impulse time domain solution (pulse-echo)
The time domain pulse-echo SV-wave response for the same void considered in the P-wave case by applying a low-pass cosine-squared windowing filter between 10 and 20 MHz to the separation of variables solution and then inverting the result into the time domain with the inverse Fourier transform.
-
1
-
0.5
0
0.5
1
1.5
-
12
-
8
-
4
0
6
time,

sec
amplitude
-
1
-
0.5
0
0.5
1
1.5
-
12
-
8
-
4
0
6
time,

sec
amplitude

## Slide 63
Flaw Scattering- SDH
Example 3: pulse-echo P-wave scattering of a cylindrical void

## Slide 64
Flaw Scattering-SDH
Recall, the scattering amplitude for the pulse-echo P-wave case was:
0
2
4
6
8
10
0
0.1
0.2
0.3
0.4
0.5
0.6
0.7
0.8
0.9

## Slide 65
Flaw Scattering- SDH
Using this separation of variables solutions at many frequencies to synthesize a P-wave impulse time domain solution (pulse-echo)
The time-domain pulse-echo P-wave response of a 0.5 mm radius cylindrical void in steel (cp = 5900 m/s, cs = 3200 m/sec) obtained by
applying a low-pass cosine-squared windowing filter between 10 and 20 MHz to the separation of variables solution and then inverting the
result into the time domain with the inverse Fourier transform.
-
1
-
0.5
0
0.5
1
1.5
-
30
-
20
-
10
0
10
20
30
time,

sec
amplitude
creeping wave
-
1
-
0.5
0
0.5
1
1.5
-
30
-
20
-
10
0
10
20
30
time,

sec
amplitude
creeping wave

## Slide 66
Flaw Scattering - SDH
Example 4: pulse-echo SV-wave scattering of a cylindrical void

## Slide 67
Flaw Scattering -SDH
Again, the scattering amplitude for the pulse-echo SV-wave case was:
0
2
4
6
8
10
0
0.2
0.4
0.6
0.8
1
1.1

## Slide 68
Flaw Scattering - SDH
Using this separation of variables solutions at many frequencies to synthesize an SV-wave impulse time domain solution (pulse-echo)
The time-domain pulse-echo SV-wave response of a 0.5 mm radius cylindrical void in steel (cp =5900 m/s, cs = 3200 m/sec) obtained by applying a low-pass cosine-squared windowing filter between 10 and 20 MHz to the separation of variables solution and then inverting the result into the time domain with the inverse Fourier transform.
-
1
-
0.5
0
0.5
1
1.5
-
40
-
30
-
20
-
10
0
10
20
30
creeping wave
time,

sec
amplitude
-
1
-
0.5
0
0.5
1
1.5
-
40
-
30
-
20
-
10
0
10
20
30
creeping wave
time,

sec
amplitude

## Slide 69
Flaw Scattering - SDH
Experimentally determined scattering amplitude by deconvolution (side-drilled hole)

## Slide 70
0
2
4
6
8
10
12
14
16
18
20
0
0.1
0.2
0.3
0.4
0.5
0.6
0.7
0.8
0.9
frequency, MHz
|A/L|
Flaw Scattering -SDH