## Slide 1
Waves Used in NDE

## Slide 2
Learning Objectives
Bulk Compressional, Shear Waves
Rayleigh (surface) waves
Lamb (plate) waves

## Slide 3
Compressional and Shear Wave Contact Transducers
fluid couplant
"solid" couplant
P-wave transducer
S-wave transducer

## Slide 4
Angle Beam Shear Wave Transducer
weld inspections
P-wave crystal and backing
plastic wedge
reflected
P- and S-waves
(suppressed)
SV-wave

## Slide 5
incident
P-wave
reflected
P-wave
transmitted
P-wave (

transmitted
S-wave (


x
y

2
c
p2
c
s2

1
c
p1
,
,
,

p2

s2

p1
p1

fluid
solid
v
p
inc
v
p
reflt
v
p
trans
v
s
trans
Generalized
Snell's law:
Mode Conversion

## Slide 6
P
P
S
P
S
P
inhomogeneous
P-wave
inhomogeneous
P, S waves
Critical Angles
p1
p1
p1

## Slide 7
stress-free surface
Rayleigh (Surface)Wave Transducer
In the late 1800's Lord Rayleigh looked for a wave
confined near the stress-free surface of an elastic solid
of the form:
Rayleigh wave
angle chosen such that

## Slide 8
x
y
By satisfying the equations of motion
and the stress-free boundary
conditions
on y = 0
Rayleigh found that the wave speed, c, must satisfy

## Slide 9
Rayleigh's equation
There is always one real root of this equation,
where
Poisson's ratio
The Rayleigh wave travels about 90% of the shear wave speed
A good approximation of this root is:

## Slide 10
ux
uy
uy
ux
xx
yy ,
xy
yy
xx
xy
displacements
stresses
The depth of penetration is a function of the frequency

## Slide 11
f … frequency
(rad/sec)
2h
If one looks for solutions of the form
Lamb (Plate) Waves

## Slide 12
then solutions of the following two types are found:
extensional waves
flexural waves
10
10
x
y
2h
(b)
(a)

## Slide 13
+ … extensional waves
- … flexural waves
satisfying the boundary conditions
on
gives the Rayleigh-Lamb equations:
There are multiple solutions of these equations. For each
solution the wave speed, c, is a different function of
frequency. Each of these different solutions is called a "mode"
of the plate.

## Slide 14
consider the extensional waves
If we let
(high frequency)
then both tanh functions are
and we find
so we just have Rayleigh waves on both stress-free surfaces:

## Slide 15
In contrast for kh <<1 (low frequency)
we find
and the Rayleigh-Lamb equation reduces to
which can be solved for c to give

## Slide 16
frequency-thickness (MHz-mm)
phase
velocity
(m/s)
fundamental
extensional
mode
fundamental
flexural
mode
c
c = cR
c = cplate