## Slide 1
Wave Propagation Fundamentals -3
Ultrasonic Attenuation

## Slide 2
Learning Objectives
Attenuation definitions
Simple method for measuring average attenuation
Model-based approach for determining attenuation
as a function of frequency

## Slide 3
Ultrasonic Attenuation
A1
A2
attenuating
medium
d
attenuation (Np/unit length)
plane wave amplitudes:

## Slide 4
Example: water
Attenuation is affected by many variables so that
generally it is not possible to give generic values
that are useful for quantitative analyses.
Thus, attenuation generally must be obtained
experimentally for the material in question
When attenuation values are quoted they are often
given as average values in decibels/unit length

## Slide 5
A2
A1
average attenuation (Np/l)
average attenuation (dB/l)
d
plane wave
pulse traveling
in an attenuative
medium:

## Slide 6
To model the effects of attenuation on the characteristics of a signal, we must be able to find the attenuation of a material as a function of frequency. However, in some applications we may be content to obtain an average attenuation value which describes the overall behavior of the amplitude of the signal. We can obtain such the average attenuation of a solid sample, for example, by using the pulse-echo setup shown.
D
On the oscilloscope screen we will see a series of evenly spaced pulses that are decreasing in amplitude. These are the waves that have been reflected from the back surface of the block one or more times.
Simple method to determine average attenuation

## Slide 7
A1
A2
A3
A4
Let the measured amplitudes of these signals be A1, A2, … etc. as shown
If the back surface of the block is in the far-field of the transducer, the incident and reflected waves will behave like attenuated spherical waves so we could express the voltage of these signals, v(t), in the form:
where the waveform shape is given by the g(t) function and is the average attenuation of the block (in Np/l)

## Slide 8
If we let gmax be the maximum amplitude of the g function then the amplitudes shown
are given by
If we take the ratio of the first two reflections we have

## Slide 9
Now
which gives

## Slide 10
Measurement of attenuation as a function of frequency
D1
D2
a
v0
material
to be measured
system function
acoustic/elastic transfer functions that describe the waves received from the front and back surface reflections
voltages received from front, back surface reflections

## Slide 11
plane wave reflection, transmission coefficients
(normal incidence)
front surface transfer function
ideal transfer
function model
plane wave reflection coefficient
back surface transfer function
ideal transfer
function model

## Slide 12
diffraction coefficient
In the back surface signal, the distance D appearing
in the diffraction correction is:

## Slide 13
measure
model
usually fit to a simple polynomial
function of frequency over the
bandwidth of the system

## Slide 14
Remarks:
To measure attenuation, it is not necessary to measure
the system function (it cancels out).
Setup shown is for measurement of P-wave attenuation.
S-wave attenuation measurements must be done in
a different setup.
This approach is ad-hoc. Actual mechanisms of
attenuation are rather complex.
For high attenuation, wave speed as well as amplitude
is affected (material dispersion).