PART 1 - GENERAL

1.01	RELATED DOCUMENTS

A.	Drawings and general provisions of the Contract, including General and Supplementary Conditions and Division 1 Specification Sections, apply to this Section.

1.02	SUMMARY

A.		This Section includes the following:

ADJUST LIST BELOW TO SUIT PROJECT.

1.	Expansion and contraction joints within portland cement concrete pavement.

2.	Joints between portland cement concrete and asphalt pavement.

B.		Related Sections include the following:

LIST BELOW ONLY CONSTRUCTION THAT THE READER MIGHT EXPECT TO FIND IN THIS SECTION BUT IS SPECIFIED ELSEWHERE.

1.	Division 2 Section "Portland Cement Concrete Paving" for constructing joints in concrete paving.

1.03	SUBMITTALS

A.		Product Data: For each joint-sealant product indicated.

B.	Samples for Verification: For each type and color of joint sealant required.  Install joint-sealant samples in 1/2-inch-wide joints formed between two 6-inch-long strips of material matching the appearance of exposed surfaces adjacent to joint sealants.

C.	Product Certificates: Signed by manufacturers of joint sealants certifying that products furnished comply with requirements and are suitable for the use indicated.

DELETE PARA BELOW IF NEITHER INSTALLER NOR TESTING AGENCY QUALIFICATIONS ARE RETAINED IN "QUALITY ASSURANCE" ARTICLE.

D.	Qualification Data: For firms and persons specified in "Quality Assurance" Article to demonstrate their capabilities and experience.  Include lists of completed projects with project names and addresses, names and addresses of architects and owners, and other information specified.

DELETE BOTH TEST REPORTS BELOW IF NOT REQUIRED FOR PROJECT.  CORRELATE WITH TESTING REQUIREMENTS IN "QUALITY ASSURANCE" ARTICLE.

E.	Compatibility and Adhesion Test Reports: From joint sealant manufacturer indicating the following:

1.	Materials forming joint substrates and joint-sealant backer materials have been tested for compatibility and adhesion with joint sealants.

2.	Interpretation of test results and written recommendations for primers and substrate preparation needed for adhesion.

1.04	QUALITY ASSURANCE

IF A MFR'S WARRANTY IS SPECIFIED REQUIRING MFR'S APPROVAL OR LICENSING OF INSTALLER, REVISE PARA BELOW ACCORDINGLY.

A.	Installer Qualifications: An experienced installer who has specialized in installing joint sealants similar in material, design, and extent to those indicated for this Project and whose work has resulted in joint-sealant installations with a record of successful in-service performance.

B.	Source Limitations: Obtain each type of joint sealant through one source from a single manufacturer.

DELETE PARA BELOW IF NOT REQUIRED.  SOME MFRS DO THEIR OWN TESTING AND MAY DECLINE TO USE AN INDEPENDENT TESTING AGENCY.

  - DELIVERY, STORAGE, AND HANDLING

A.	Deliver materials to Project site in original unopened containers or bundles with labels indicating manufacturer, product name and designation, color, expiration date, pot life, curing time, and mixing instructions for multicomponent materials.

B.	Store and handle materials to comply with manufacturer's written instructions to prevent their deterioration or damage due to moisture, high or low temperatures, contaminants, or other causes.

1.06	PROJECT CONDITIONS

A.	Environmental Limitations: Do not proceed with installation of joint sealants under the following conditions:

1.	When ambient and substrate temperature conditions are outside limits permitted by joint sealant manufacturer.

DELETE SUBPARA ABOVE OR BELOW.

2.	When ambient and substrate temperature conditions are outside limits permitted by joint sealant manufacturer or are below 40 deg F.

3.	When joint substrates are wet.

B.	Joint-Width Conditions: Do not proceed with installation of joint sealants where joint widths are less than that allowed by joint sealant manufacturer for application indicated.

C.	Joint-Substrate Conditions: Do not proceed with installation of joint sealants until contaminants capable of interfering with their adhesion are removed from joint substrates.

PART 2 - PRODUCTS

2.01	MATERIALS, GENERAL

A.	Compatibility: Provide joint sealants, backing materials, and other related materials that are compatible with one another and with joint substrates under conditions of service and application, as demonstrated by joint sealant manufacturer based on testing and field experience.

DELETE PARAS BELOW IF SEALANTS SPECIFIED ARE NOT OFFERED IN A CHOICE OF COLORS, WHICH IS THE CASE WITH MOST PAVEMENT JOINT SEALANTS.

B.	Colors of Exposed Joint Sealants: As selected by Architect from manufacturer's full range for this characteristic.

2.02	COLD-APPLIED JOINT SEALANTS

A.	Type SL Silicone Sealant for Concrete and Asphalt: Single-component, low-modulus, neutral-curing, self-leveling silicone sealant complying with ASTM D 5893 for Type SL.

B.	Multicomponent Low-Modulus Sealant for Concrete and Asphalt: Proprietary formulation consisting of reactive petropolymer and activator components producing a pourable, self-leveling sealant.

C.	Available Products: Subject to compliance with requirements, cold-applied joint sealants that may be incorporated into the Work include, but are not limited to, the following:

RETAIN ABOVE FOR NONPROPRIETARY OR BELOW FOR SEMIPROPRIETARY SPECIFICATION.  REFER TO DIVISION 1 SECTION "MATERIALS AND EQUIPMENT."

1.	Type SL Silicone Sealant for Concrete and Asphalt:

a.	890-SL; Dow Corning.

2.	Multicomponent Low-Modulus Sealant for Concrete and Asphalt:

a.	SOF-SEAL; W.R. Meadows, Inc.

2.03	JOINT-SEALANT BACKER MATERIALS

A.	General: Provide joint-sealant backer materials that are nonstaining; are compatible with joint substrates, sealants, primers, and other joint fillers; and are approved for applications indicated by joint sealant manufacturer based on field experience and laboratory testing.

RETAIN PARA BELOW FOR USE OF COLD- AND HOT-APPLIED SEALANTS IN JOINTS, SUCH AS CONTRACTION JOINTS, WHERE BACKER MATERIALS SERVE ONLY TO LIMIT SEALANT DEPTH AND PREVENT BOTTOM-SIDE ADHESION.

B.	Round Backer Rod for Cold- and Hot-Applied Sealants: ASTM D 5249, Type 1, of diameter and density required to control sealant depths and prevent bottom-side adhesion of sealant.

RETAIN PARA BELOW FOR USE OF COLD- AND HOT-APPLIED SEALANTS IN JOINTS, SUCH AS EXPANSION JOINTS, WHERE IT IS DESIRABLE FOR BACKING MATERIAL TO FILL REMAINDER OF JOINT OPENING UNDER SEALANT AND MINIMIZE ACCUMULATION OF WATER AND INCOMPRESSIBLE MATERIALS.

C.	Backer Strips for Cold- and Hot-Applied Sealants: ASTM D 5249; Type 2; of thickness and width required to control sealant depths, prevent bottom-side adhesion of sealant, and fill remainder of joint opening under sealant.

D.	Round Backer Rods for Cold-Applied Sealants: ASTM D 5249, Type 3, of diameter and density required to control sealant depths and prevent bottom-side adhesion of sealant.

2.04	PRIMERS

GENERALLY RETAIN BELOW UNLESS IT IS KNOWN THAT PRIMING OF SUBSTRATES IS NOT REQUIRED WITH SEALANTS SPECIFIED.  PURPOSE OF PRIMERS IS TO IMPROVE ADHESION OF SEALANT TO SUBSTRATE.

A.	Primers: Product recommended by joint sealant manufacturer where required for adhesion of sealant to joint substrates indicated, as determined from preconstruction joint- sealant-substrate tests and field tests.

PART 3 - EXECUTION

3.01	EXAMINATION

A.	Examine joints indicated to receive joint sealants, with Installer present, for compliance with requirements for joint configuration, installation tolerances, and other conditions affecting joint-sealant performance.

B.		Proceed with installation only after unsatisfactory conditions have been corrected.

3.02	PREPARATION

A.	Surface Cleaning of Joints: Clean out joints immediately before installing joint sealants to comply with joint sealant manufacturer's written instructions.

AS PREVIOUSLY NOTED IN "PRIMERS" ARTICLE, PURPOSE OF PRIMERS IS TO IMPROVE ADHESION OF SEALANT TO SUBSTRATE.

B.	Joint Priming: Prime joint substrates where indicated or where recommended in writing by joint sealant manufacturer, based on preconstruction joint-sealant-substrate tests or prior experience.  Apply primer to comply with joint sealant manufacturer's written instructions.  Confine primers to areas of joint-sealant bond; do not allow spillage or migration onto adjoining surfaces.

3.03	INSTALLATION OF JOINT SEALANTS

A.	General: Comply with joint sealant manufacturer's written installation instructions applicable to products and applications indicated, unless more stringent requirements apply.

B.	Sealant Installation Standard: Comply with recommendations of ASTM C 1193 for use of joint sealants as applicable to materials, applications, and conditions indicated.

C.	Install backer materials of type indicated to support sealants during application and at position required to produce cross-sectional shapes and depths of installed sealants relative to joint widths that allow optimum sealant movement capability.

1.	Do not leave gaps between ends of backer materials.

2.	Do not stretch, twist, puncture, or tear backer materials.

3.	Remove absorbent backer materials that have become wet before sealant application and replace them with dry materials.

D.	Install sealants by proven techniques to comply with the following and at the same time backings are installed:

1.	Place sealants so they directly contact and fully wet joint substrates.

2.	Completely fill recesses provided for each joint configuration.

3.	Produce uniform, cross-sectional shapes and depths relative to joint widths that allow optimum sealant movement capability.

E.	Tooling of Nonsag Sealants: Immediately after sealant application and before skinning or curing begins, tool sealants according to requirements specified below to form smooth, uniform beads of configuration indicated; to eliminate air pockets; and to ensure contact and adhesion of sealant with sides of joint.

1.	Remove excess sealants from surfaces adjacent to joint.

2.	Use tooling agents that are approved in writing by joint sealant manufacturer and that do not discolor sealants or adjacent surfaces.

F.	Provide joint configuration to comply with joint sealant manufacturer's written instructions, unless otherwise indicated.

3.04	CLEANING

A.	Clean off excess sealants or sealant smears adjacent to joints as the Work progresses by methods and with cleaning materials approved by manufacturers of joint sealants and of products in which joints occur.

3.05	PROTECTION

A.	Protect joint sealants during and after curing period from contact with contaminating substances and from damage resulting from construction operations or other causes so sealants are without deterioration or damage at time of Substantial Completion.  If, despite such protection, damage or deterioration occurs, cut out and remove damaged or deteriorated joint sealants immediately so installations with repaired areas are indistinguishable from the original work.

END OF SECTION 02764