PART I - GENERAL

  - SCOPE

- Provide all materials, equipment, incidentals and labor for patching, finishing, curing and protecting from flowing water and mechanical injury the concrete specified.

  - RELATED WORK

- Cast-In-Place Concrete - Section 03300

  - REFERENCED STANDARDS FOR QUALITY ASSURANCE

- All work shall be in accordance with the applicable sections and references therein, of the Specifications and Standards of the following:

- American Concrete Institute (ACI)

- American Society For Testing Materials (ASTM)

- In conflicts between this specification, industry standards and/or local building codes, the more stringent requirements shall govern.

  - SUBMITTALS

- Product data on curing compounds.

PART II - PRODUCTS

  - WATER CURING

- Heavy burlap weighing at least 10 ounces per square yard.

- Clean river sand, ASTM C-33.

- Sawdust

  - MEMBRANE CURING

A.	Waterproof sheet material conforming to ASTM C-171, Standard Specification for Sheet Materials For Curing Concrete.

  - LIQUID CURING

- "Kure-N-Seal"  	Sonneborn

- "Clear Bond"		Guardian Chemical

- "Clear Seal"          	(A.C. Horn) Grace Construction

- "Encocure" or Kurez E-100"         	Euclid Chemical Co.

- "Clear Seal"         	Lambert Corporation

- "Chem-Seal"           	Hillyard Chemical Co.

- "Masterseal"          		Master Builders

PART III - EXECUTION

- PATCHING OF CONCRETE

- Immediately after removing forms, all surfaces shall be inspected for defective work.  Any concrete which is poorly formed, out of alignment or level, or shows a defective service, shall at the election of the Engineer, be removed from the job by the Contractor at the Contractor's expense.  The engineer may grant permission to patch or repair defective work; but such permission shall not be considered a waiver of the Engineer's right to require complete removal of the defective work, if in the Engineer's opinion, the patching or repairs do not satisfactorily restore the quality and appearance of the items in question.

- Where permitted by the Engineer, all honeycombs, voids, stone pockets, tie holes and other defective areas shall be patched as soon as practicable.  Patching shall be done in accordance with the following procedure.

- Defective areas shall be chipped away to a depth of at least 1" with the edges cut perpendicular to the surface.

- The area to be patched and space at least 6" wide entirely surrounding it shall be wetted to prevent absorption of water from the patching mortar.

- A grout of equal parts of Portland Cement and sand, with sufficient water to produce a brushing consistency, shall be well brushed into the surface followed immediately by the patching mortar.

- The patch shall be made of the same materials and of approximately the same proportion as used for the concrete except that the coarse aggregate shall be omitted.  The mortar shall not be richer than 1 part cement to 3 parts sand.  The proportions of white and gray cements shall be determined by making a trial patch.  The amount of mixing water used shall be the minimum consistent with the requirements of handling and placing.  The mortar shall be retempered without the addition of water by allowing it to stand for one hour, during which time it shall be mixed with a trowel to prevent setting.

- The mortar shall be thoroughly compacted into place and screened off so as to leave the patch slightly higher than the surrounding surface.  The patch shall then be left undisturbed for one to two hours to permit initial shrinkage before being finally finished.

- The patched areas shall be finished to match the adjoining surface.  On exposed surfaces, where unlined forms have been used, the final finish shall be obtained by striking off the surface with a straight edge spanning the patch and held parallel to the form marks.

- Curing of the patched areas shall be in accordance with these specifications.

- Contractor's Option:

In lieu of mixing grout for patching, the Contractor may provide a PVC bonding agent recommended by the manufacturer for the use intended.  Approved products and manufacturers:

- "Dara Weld C" by W.R. Grace

- "Weldcrete" by E.A. Larson

- "Vinyl Hesive" by Nox-Crete

- CONCRETE FLOORS

(All floors, suspended slabs, and slabs on grade)

- The surface of all concrete shall be worked with a wood float or by machine in a manner which will compact the concrete and produce a surface free of depressions or inequalities of any kind.  Test for grade (or level) and correct as necessary by removing excess or adding and compacting additional concrete.  After the concrete has hardened sufficiently to prevent fine material from working to the top (when the sheen or shiny film of water on the surface has disappeared), the surface shall be finished in accordance with the applicable following paragraphs, but excessive working shall be avoided.  Final finishing shall not be started until all surface water has disappeared.  The drying of the surface moisture must proceed naturally and must not be hastened by sacking or dusting-on of dry sand and/or cement.

- After finishing concrete floors, and before traffic is allowed over them, the floors shall be covered with one layer of Sisal Kraft or approved similar heavy waterproof paper lapped at least 4" with lap continuously filled with waterproof cement.  In case of damage or injury to the paper, it shall be replaced immediately.  It is the intent of this specification to protect the floors for acceptance by the Engineer.  At the end of the job, or just prior to application of permanent floor coverings, slabs shall be thoroughly cleaned and left in suitable condition for installation of permanent covering.

- Tolerances

- While still plastic, concrete surfaces shall be testing for surface irregularities with a 10' straightedge and the necessary corrections made. Allowable irregularities is 1/8" in 10', non-accumulating.

- Slab surfaces to receive topping or setting bed, 1/4" to 10'.

- Floor slab surfaces shall slope uniformly to floor drains as shown on the drawings.

D.	Monolithic finish for Slabs

All interior floor slabs shall have a steel trowel finish (except for floor slabs to receive ceramic tile).  The steel troweling shall produce a smooth finished surface free of pin holes and other imperfections.

E.	Depressed slabs shall have a rough screed finish at levels indicated on the drawings.

F.	Broom finish shall be used for all interior stairs unless shown otherwise.  Slabs and landings shall be troweled to a smooth, even surface and receive a light broom finish.

- FINISHES ON FORMED CONCRETE SURFACES

- Common finish shall be confined to concrete surfaces which will be covered by other construction and which will not be visible.  This finish shall be produced by filling smoothly all tie holes, honeycomb and other depressions, knocking off and evening-up burrs and form marks.

- CURING AND SEALING COMPUND APPLICATION

- Curing and sealing compound shall be applied as soon as the concrete has set sufficiently so as not to be marred by the application.  Preparation of surfaces, quantities used, application procedures, and installation precautions shall be followed in strict compliance with the manufacturer's stated recommendations and directions as set forth on the package.

- Final curing shall continue for 7-days minimum.

## END OF SECTION