## PART I - GENERAL

  - SCOPE

- This section covers all items fabricated from metal shapes, plates, sheets or rods and all other wrought metal for use in support of piping.

- Fabricated metal items, which are detailed on the drawings but not mentioned specifically herein, shall be fabricated in accordance with the applicable requirements of this section

  - QUALITY ASSURANCE

- Regulations, References and Standards: The latest edition of the following regulations, standards, etc. are hereby included in and made part of these specifications.

- American Institute of Steel Construction (AISC): "Specification for the Design, Fabrication, and Erection of Structural Steel for Buildings".  "Code of Standard Practice for Steel Buildings and Bridges".  This code shall be available at all times for reference.

- American Society for Testing and Materials (ASTM):  "Standard Specification for Structural Steel" designation A-36, and "Specifications for Structural Joints" using ASTM A-325.

- American Welding Society (AWS):  "Code for Welding in Building Construction" AWS D1.0-69, and all ARC welding electrodes shall meet the provisions of Section 412, 417 or 418 of AWS D1.0-69 as applicable.

  - SUBMITTALS

Submit shop drawings showing all material and connections of all items for approval.

## PART II - PRODUCTS

  - BASIC MATERIALS

- All materials shall be new and undamaged and shall conform to pertinent AISC, ANSI, ASTM or other industry standards.  Unless specified otherwise in other specification all sections, materials in fabricated metal items shall conform to the following requirements:

- Steel

  - Plates and Shapes		ASTM A 36

  - Pipe					ASTM A 53, Grade B, seamless

  - Bolts

High Strength		ASTM A 325

Flat Washers		ANSI B27.2

- ARC welding electrodes shall be E70 series (AWS). Grade C, Class

- Shop Coat Paint - Refer to Section 15050.

  - FABRICATION

- All members shall be free from twist, bends, buckles, or open joints.  Parts assembled with bolts shall be in close contact, except where separators are required.  All members shall be so accurately made and spaced that when assembled, the parts shall come together and bolts enter without distortion.

- Connections Standard AISC, latest edition, specifications shall be used in determining the connections, unless otherwise shown on the drawings, including the number of bolts and spacing required.  All connections shall be bolted or welded and shall not interfere with architectural clearances.  The best shop practices shall be followed for shearing, punching, diameter of bolt holes, spacing machine riveting, welding, etc.

- Bearing surfaces shall be planed to true beds.  Abutting surfaces shall be closely fitted. Tubular sections shall be completely seal-welded at all joints and seams.

- Structural Steel shall be provided with all holes for attaching pipe attachments.

- Steel requiring accurate alignment shall be provided with slotted holes and/or washers for aligning the Steel accurately.  No erection bolts or other fastening parts or joints or rolled stamping names shall show on finished surfaces of exposed Steel, exterior or interior.

- Welding - All welding except to existing Steel shall be performed in shop.  Refer to Section 15050.

PART III - EXECUTION

  - ERECTION, INSTALLATION AND APPLICATION

- Erection shall include the setting and erection of all Structural Steel.  The frame shall be erected true and plumb.   Temporary bracing shall be used wherever necessary to take care of all loads to which the structure may be required for safety.  As erection progresses, the work shall be securely bolted up to take care of all dead load, wind and erection stresses.  Steel shall be erected level or plumb within a tolerance as recommended by AISC Code of Standard Practice.

- No final bolting or welding shall be done until each portion of the structure has been properly aligned.  Bolting shall be done with high strength friction type bolts and hardened washers, using properly calibrated and inspected torque tension wrenches.  Bolts marked after tightening.  Bolts shall be drawn-up tight and threads set so that nuts cannot become loose.  Set high-strength bolts by the turn-of-the-nut method.  Holes for turned bolts to be inserted in the field shall be reamed in the field.  Erection bolts are not to be used on exposed surfaces.  Erection bolts or other surfaces and stiffeners shall not interfere with architectural clearances.

- Protect all adjacent finished surfaces during the progress of welding.  Damaged surfaces shall be replaced at the cost of the erection contractor.

  - FIELD QUALITY CONTROL

- Field errors shall not be corrected by burning, except with the permission of the engineer.

- Inspection for tightness shall be the arbitration inspection method.

# END OF SECTION