# PART I – GENERAL

  - WORK INCLUDED

- Sub-grade preparation.

- Crushed stone or crushed gravel compacted base course.

  - RELATED WORK

- Section 02514 – Portland Cement Concrete Paving

- Section 02511 – Hot Mix Asphalt Paving

  - REFERENCES

- Where Tennessee Department of Transportation Specifications for road and Bridge construction are referred to, the applicable requirements of that Section shall be considered a part of these specifications and all materials and construction methods prescribed therein shall be as binding as if herein specified.  The Sections referred to are from Tennessee, current edition with latest supplements.

## PART II – PRODUCTS

  - MATERIALS

- Base Courses: Comply with Tennessee Department of Transportation specifications, Section 303, Class A.

## PART III – EXECUTION

  - SUB-GRADE PREPARATION

- Grade sub-grade to lines and grades indicated.  Preparation of sub-grade shall be in compliance with Tennessee D.O.T. Specifications sections referenced herein.

  - BASE COURSE

- Construct crushed stone or crushed gravel base course to thickness indicated on drawings and in compliance with Tennessee D.O.T. Specifications, Section 303, Class A.

- All areas to receive paving shall be graded to the indicated sub-grade elevation and proof-rolled as outlined below.

- All areas (sub-grade) to receive compacted fill, pavements or slabs on grade shall be proof-rolled in the presence of the Owner’s Representative or Testing Agency to detect any soft areas that may exist.  A four-wheeled, pneumatic-tired roller of not less than 25 tons, or its equivalent, shall be used for this operation.  At least four passes shall be made, two in each of two directions at right angles.  Any soft areas thus disclosed shall be stabilized or undercut and replaced with properly compacted material as approved by the Owner’s Representative or Testing Agency.

- Proof-rolling should be conducted only on soils in their approximate natural moisture condition.  Proof-rolling should not be undertaken after rains while soils are still in a high moisture condition (well above the natural moisture content) or on soils which are desiccated by prolonged drying.

### END OF SECTION