# PART I – GENERAL

  - WORK INCLUDED

- Concrete sidewalks, roads, aprons, door pads, curbs and gutters.

- Reinforcement.

- Surface finish.

- Curing.

  - RELATED WORK

- Section 02512 - Sub-grade and Base Course Preparation

- Section 02764 - Pavement Joint Sealants

- Section 02300 – Earthwork

- Division 3 Section “Cast-in-Place Concrete”

  - REFERENCES

- ACI 211.1	-	Recommended Practice for Selecting Proportions for Normal and Heavyweight Concrete.

- ACI 211.2	-	Recommended practice for Selecting Proportions for Structural Lightweight Concrete.

- ACI 301	-	Specifications for Structural Concrete for Buildings.

- ACI 304R	-	Guide for Measuring, Mixing, Transporting and Placing Concrete.

- ACI 305R	-	Hot Weather Concreting.

- ACI 306R	-	Cold Weather Concreting.

- ACI 315	-	Details and Detailing of Concrete Reinforcement.

- ACI 318	-	Building Code Requirements for Reinforced Concrete.

- ACI 347	-	Recommended Practice for Concrete Formwork, Concrete Reinforcing Steel Institute, Manual of Standard Practice.

- ASTM A185	-	Welded Steel Wire Fabric for Concrete Reinforcement.

- ASTM A497	-	Welded Deformed Steel Wire Fabric for Concrete Reinforcement.

- ASTM A615	-	Deformed and Plain Billet-Steel for Concrete Reinforcement.

- ASTM C31	-	Standard Method of Making and Curing Concrete Test Specimens in the Field.

- ASTM C33	-	Standard Specification for Concrete Aggregates.

- ASTM C39	-	Standard Test Method of Compressive Strength of Cylindrical Concrete Specimens.

- ASTM C78	-	Flexural Strength of Concrete (Using Simple Beam with Third-Point Loading).

- ASTM C94	-	Ready Mixed Concrete.

- ASTM C143	-	Slump of Portland Cement Concrete.

- ASTM C150	-	Portland Cement.

- ASTM C172	-	Sampling Fresh Concrete.

- ASTM C173	-	Air Content of Freshly Mixed Concrete by the Volumetric Method.

- ASTM C192	-	Making and Curing Concrete Test Specimens in the Laboratory.

- ASTM C231	-	Air Content Of Freshly Mixed Concrete by the Pressure Method.

- ASTM C260	-	Air-Entraining Admixtures for Concrete.

- ASTM C309	-	Liquid Membrane-Forming Compounds for Curing Concrete.

- ASTM C494	-	Chemical Admixtures for Concrete.

- ASTM D1751	-	Preformed Expansion Joint Fillers for Concrete Paving and Structural Construction.

- ASTM D1752	-	Preformed Sponge Rubber and Cork Expansion Joint Fillers for Concrete Paving and Structural Construction.

- Tennessee Department of Transportation – Standard Specifications for Road and Bridge Construction.

  - QUALITY ASSURANCE

- Perform work in accordance with ACI 301.

- Obtain materials from same source throughout.

- Submit laboratory test reports for concrete materials and mix design test as specified.

- Provide material certificates in lieu of materials laboratory test reports when permitted by Owner’s Representative.  Material certificates shall be signed by manufacturer and Contractor, certifying that each material item meets specified requirements.

  - TESTS

- As the work progresses, sample concrete in accordance with ASTM C172.

- Make slump tests according to ASTM C143, one slump test for each set of test cylinders.

- Test air content of concrete made with normal-weight aggregates having low water absorption according to either ASTM C231 or ASTM C173.  For lightweight aggregates or aggregates with high absorptions, use latter test method.

- Make compression test specimens and cure according to ASTM C31.  Each test shall consist of one set of laboratory cured cylinders.  A set shall consist of four cylinders.  Minimum number of tests shall be one for 100 cubic yards of concrete for each class.  Make at least one test per day of each class of concrete used that day.

- Cure specimens under laboratory conditions.  Specimens cured under job conditions may be required when, in Owner’s Representative’s opinion, there is a possibility of the surrounding air temperature falling below 40F, or rising above 90F.

- Test cylinders according to ASTM C39.

- Test laboratory cured cylinders one at seven days, two at 28 days, and one at 56 days, if required.

- Strength level of concrete will be considered satisfactory if averages of any three consecutive strength test results of laboratory cured cylinders equal or exceed specified strength f’c, and no individual strength test result falls below specified strength f’c by more than 500 psi.

- Make reports on cylinder tests to Owner’s Representative and show dates placed and tested, name of job, proportions of cement and aggregate, quantity of water, slump, air content, admixtures, location of concrete in the project, type of concrete, compressive strength in pounds per square inch and atmospheric and concrete temperature at time of sampling.

- In cases where strength of laboratory cured cylinders shown by tests for any portion of paving falls below required compressive strengths specified, Owner’s Representative shall have the right to order change in mix or in cement content for remaining portion of the paving.

- Make and cure flexural test beam specimens according to ASTM C78.  Each test shall consist of one set of laboratory cured beams.  A set shall consist of two beams.  Minimum number of tests shall be one for each 100 cubic yards of concrete placed, at least one per day.  Cure specimens under laboratory conditions.

- Test beams according to ASTM C78, simple beam with third-point loading.  Test beams shall have six inch by six inch cross-section.

- Test beams at 14 days.

- Flexural strength level of concrete shall be considered satisfactory as long as averages of any three consecutive test results of laboratory cured beams equal or exceed specified strength, and no individual strength test result falls below specified strength by more than 100 psi.

- Concrete cylinder and flexural tests shall be made by an independent testing laboratory selected by Owner.  Cost of initial tests shall be paid for by Owner.  Subsequent tests required as a result of improper strength shall be paid for by Contractor.

## PART II – MATERIALS

  - CONCRETE MATERIALS

- Cement: ASTM C150, Normal-Type I, gray color.

- Fine and Coarse Aggregates: ASTM C33.  Provide aggregates from single source for exposed concrete.

- For grading tests of fine and coarse aggregates, use square mesh wire cloth complying with ASTM E11.

- Fine Aggregate:

- Provide washed natural sand of strong, hard durable particles.

- Grade from coarse to fine within following limits:

| Sieve | Percentage by Weight Passing Sieve |  |
| --- | --- | --- |
| Size | Minimum | Maximum |
| 3/8” | 100 | --- |
| No. 4 | 95 | 100 |
| No. 8 | 65 | 95 |
| No. 16 | 45 | 75 |
| No. 30 | 30 | 50 |
| No. 50 | 10 | 22 |
| No. 100 | 2 | 8 |

3.  Coarse Aggregate:

- Provide coarse aggregate consisting of clean, hard, fine-grained, sound crushed rock or washed gravel, or combination of both.

- Any piece having length in excess of five times average thickness shall be considered flat or elongated.

- The maximum size coarse aggregate shall 1½ “ with the minimum size being 1 inch.

- Grade combined aggregates within following limits:

|  | Sieve Size or Percentage by Weight Passing Sieve |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Size in Inches |  | 1½” Aggregate |  |  | 1” Aggregate |  |  |
| 1 ½” |  | Min. |  | Max. | Min. |  | Max |  |
| 1½” |  | 95 |  | --- | --- |  | --- |  |
| 1” |  | 75 |  | 90 | 90 |  | 100 |  |
| ¾” |  | 55 |  | 77 | 70 |  | 90 |  |
| 3/8” |  | 40 |  | 55 | 45 |  | 65 |  |
| No. 4 |  | 30 |  | 0 | 31 |  | 7 |  |
| No. 8 |  | 22 |  | 35 | 23 |  | 40 |  |
| No. 16 |  | 16 |  | 30 | 17 |  | 35 |  |
| No. 30 |  | 0 |  | 20 | 10 |  | 23 |  |
| No. 50 |  | 2 |  | 8 | 2 |  | 10 |  |
| No. 100 |  | 0 |  | 3 | 0 |  | 3 |  |

- Water: Clean, not detrimental to concrete, and conforming to ACI 318, Article 3.4.

- Form Materials.

- Conform to ACI 301.

C.   	Reinforcement

- Reinforcing Steel:  ASTM A615; 60 ksi yield grade; deformed billet steel bars.

- Welded Steel Wire Fabric: Plain type, ANSI/ASTM A185; in flat sheets; uncoated finish.

- Tie Wire:  Annealed steel, minimum 16 gauge size.

- Dowels: ASTM A615; 40 ksi yield grade, plain steel, uncoated finish.

D.	Accessories

- Curing Compound: FS TT-C-800, Type 1, 30% solids; ASTM C309, Kurey DR, manufactured by Euclid Chemical Company and L&M Cure Resin by L&M Construction Materials, or approved equal.

- Expansion Joint Filler:  Non-extruding, non-bituminous, resilient type complying with AASHTO M153 and ASTM D1752.

- Joint Sealant for Pavements Unless Noted Otherwise on Drawings: Urethane complying with ASTM D1850 and ASTM C290 such as “Urexpan NR-200” by Pecora Corp., “VULKEM-245” by Mameco International, or approved equal.

- Admixtures

- Air Entrainment: Conform to ASTM C260.

- Water Reducing Admixture: Conform to ASTM C494, Type A, containing not more than 1% chloride ions.

- High Range Water Reducing Admixture (Super Plasticizer): Conform to ASTM C494, Type F or G, containing not more than 1% chloride ions.

- Non-Chloride Accelerator Admixture: Conform to ASTM C494, Type C or E.  Provide long-term test data proving non-corrosive effect on reinforcing steel.

- Concrete Mix Design

- Design concrete for flexural strength of 650 pounds per square inch at 14 days, compressive strength of (f’c) of 4,500 pounds per square inch at 28 days.

- Unless otherwise noted, concrete shall have minimum cement content of 517 pounds per cubic yard of concrete and maximum water content not exceeding 28.0 gallons per cubic yard.

- Concrete shall contain no calcium chloride nor shall admixtures contain more than 1 % chloride ions or air entraining cement, unless approved by Owner’s Representative.

- Concrete shall be air entrained and conform to air content limits of Table 1 below.

| Table 1 – Air Content for Air-Entrained Concrete |  |
| --- | --- |
| Maximum Size Coarse | Air Content |
| Aggregate Inches | Percent by Volume |
| 1 | 5.5+1 |
| 1 ½” | 5.0+1 |

- Concrete shall have maximum water-cement ratio of 0.45.

- Concrete shall have a slump of 3”, plus or minus ½”.

- Methods of measuring concrete materials shall be such that proportions can be accurately controlled and easily checked.  Measurement of materials for ready-mixed concrete shall conform to ASTM C94.

- Use accelerating admixtures in cold weather only when approved by Owner’s Representative.  Use of admixtures will not relax cold weather placement requirements.

- Use set-retarding admixtures during hot weather only when approved by Owner’s Representative.

## PART III – EXECUTION

  - INSPECTION

- Verify compacted subgrade ready to support paving and imposed loads.

- Verify correct gradients and elevations of base.

- Beginning installation implies acceptance of existing conditions.

  - PREPARATION

- Moisten base to minimize absorption of water from fresh concrete.

- Notify Owner’s Representative minimum 24 hours before start of concreting operations.

  - FORMING

- Place and secure forms to correct location, dimension, and profile.

- Assemble formwork to permit easy stripping and dismantling without damaging concrete.

- Place joint fillers vertical in position, in straight lines.  Secure to formwork during concrete placement.

  - REINFORCEMENT

- Where noted on drawings, reinforce concrete paving with welded steel wire fabric.

- Provide chairs, supports, spacers, bolsters and other devices to keep reinforcement at proper elevations and in place.

- Interrupt reinforcement at control, contraction and expansion joints.

  - FORMED JOINTS

- Place joints as shown on plans to correct elevation and profile.

  - PLACING CONCRETE

- Place concrete in accordance with ACI 304R.

- Hot Weather Placement:  ACI 305R

- Cold Weather Placement:  ACI 306R

- Ensure reinforcements, inserts, embedded parts, formed joints and are not disturbed  during concrete placement.

- Place concrete continuously between predetermined construction joints.  Do not break or interrupt successive pours such that cold joints occur.

- Place concrete to pattern indicated.  Saw cut contraction joints at an optimum time after finishing.  Saw joints in accordance with details on plans.

- Chamfer exposed corners of concrete using wood, metal, PVC, or rubber chamfer strips fabricated to produce smooth lines and tight edge strips.

  - FINISHING

- Road and Apron Paving:  Light broom.

- Sidewalk Paving:  Light broom and trowel joint edges.

- Place curing compound on exposed concrete surfaces immediately after finishing.  Apply in accordance with manufacturer’s instructions.

  - FIELD QUALITY CONTROL

- Field testing will be performed by an independent testing company as selected by the Owner.

- Maintain records of placed concrete items.  Record date, location of pour, quantity, air temperature, and test samples taken.

  - PROTECTION

- Immediately after placement, protect concrete from premature drying, excessive hot or cold temperatures, and mechanical injury.

END OF SECTION