PART I - GENERAL

  - SCOPE

- This section covers formwork, rebars and all other materials, equipment and methods for mixing, placing, testing, finishing, curing, etc. all plain and reinforced, cast-in-place, normal weight concrete.

- All embedded items required by other trades under the General Construction Contract shall be set under this section.

- Items not included in the General Construction Contract shall be furnished and placed by the trade requiring these items to be embedded in concrete, but the General Contractor shall cooperate with these trades in order that they are afforded an opportunity to make their installations before concrete is placed.

  - RELATED WORK

- Concrete Curing & Finishing - Section 03305

  - REFERENCE STANDARDS FOR QUALITY ASSURANCE

- All work, testing and inspection shall be in accordance with the applicable sections, and references therein, of the Specifications and Standards of the following:

- Locally Adopted Building Code

- American Concrete Institute (ACI)

- Concrete Reinforcing Steel Institute (CRSI)

- American Society For Testing Materials (ASTM)

- PS-1-U.S. Product Standard for Softwood Plywood.

- In conflicts between this specification, industry standards and/or local building codes, the more stringent requirements shall govern.

  - SUBMITTALS

- Shop drawings for all form work where appropriate and requested.

- Shop drawings for placing of all reinforcing steel.

- A trial mix prepared by an independent testing laboratory for each class of concrete and for each size and gradation of aggregate proposed for the project.  The preliminary mix design submittals shall contain the applicable information all components of the mix.  After mix is established and approved, substitutions shall not be made.  (See Paragraph 3.07 - TESTING)

PART II - PRODUCTS

- FORMWORK

- Forms for surfaces which will be exposed to view shall be plywood, steel or lined forms meeting the architectural requirements of the project.  Metal or fiberglass forms shall be used for joist and waffle slabs.

- Form ties shall be designed by the Contractor.

- Form releasing agent shall be non-staining "Form Oil" as manufactured by Texaco, Sinclair or Nox-Crete Form Coating.

- REINFORCING STEEL

- Bars shall be deformed billet-steel bars conforming to ASTM A 615.  All bars should be grade 60.  All bars shall be shop-fabricated and bent cold.  Bars shall be free from defects and kinks and from bends not indicated on the Drawings or approved bending diagrams.

- Mesh reinforcement shall be electrically welded, plain wire fabric conforming to ASTM A 185.  Wire shall be cold-drawn mild steel conforming to ASTM A 82.

- Tie wire shall be of black annealed steel, 16-gage minimum.

- Metal accessories per CRSI.

- CONCRETE

- Cement shall be an American brand approved by the engineer, conforming to ASTM C-150, Type 1, unless another type is specified.  For exposed surface one brand shall be used throughout.

- (NOTE:  All concrete exposed to freezing and de-icing agents shall have a minimum of 564 pounds (6 bags) of cement per cubic yard with a maximum water/cement ratio of .5 lbs/lb and 5 percent entrained air.)

- Coarse aggregate shall be crushed stone or gravel having clean, hard durable uncoated particles sized within the limits of ASTM C-33, Table 2, Size No. 57.

- Fine aggregate shall be clean, hard, durable natural siliceous river sand with uncoated grains free from all organic material or other impurities meeting ASTM C-33.  Manufactured sand shall not be used.

- Mixing water shall be clean, potable, free from oil, acids, salts, alkalies and injurious amounts of vegetable matter.

- ADMIXTURES:

- All exterior concrete shall have an air-entraining agent (ASTM C-260) equal to Masterbuilders MBVR to produce a plastic mix with 6% +/- 1% of entrained air.  It shall be included in the trial design mixes submitted to the Engineer for approval.

- All interior concrete shall have an air-entraining agent (ASTM C-260) equal to Masterbuilders MBVR to produce a plastic mix with 2% - 3% of entrained air.  It shall be included in the trial design mixes submitted to the Engineer for approval.

- No other admixture shall be used without the written permission of the Architect/Engineer.

- Curing materials per Section 03305.

- JOINT FILLER

- Expansion joint filler shall be preformed resilient, non-extruding, non-bituminous, fiber type conforming to ASTM D-1751 or D-544.

- WATER STOPS

A.	Flexible polyvinyl, 3/8" X 6" ribbed type with center bulb.

PART III - EXECUTION

- FORMWORK

- Where applicable forms shall be placed according to approved shop drawings.

- Erect forms to required dimensions and cross-sections, free of surface defects, tied, shored and braced to movement and leakage of mortar.  Any defective formwork and/or defective concrete shall be removed at Contractor's expense.

- Metal and/or fiberglass pans that are bent, badly rusted, cracked or otherwise damaged shall not be used and shall be removed from the site.

- Provide forms for footings if soil or other conditions are such that earth trench forms are unsuitable.  Omission of forms shall be approved by the Architect/Engineer.

- Construct forms so they can be removed readily without hammering or prying against the concrete.

- Provide box-outs, bulkheads with keys, cleanouts, expansion joint strips, and other related items and features.

- Chamfer all exposed outside corners unless otherwise instructed.

- Tolerances shall be within the limitations set forth in ACI 347.

- FORM COATING

- Immediately before the placing of reinforcing, faces of all forms in contact with the concrete shall receive a thorough coating of the liquid form releasing agent specified, applied in compliance with the manufacturer's instructions.  After oiling, any surplus oil on the form surfaces shall be removed.

- REMOVAL OF FORMS

- No forms shall be removed without the approval of the Architect/Engineer.  In general and under normal conditions the Architect/Engineer will approve removal of forms as follows:

- Concrete beams, slabs and other members which span between definite supports shall attain 70% of the specified 28-day strength before removal of the forms.  Shores for cantilevered beams and slabs shall remain in place for at least an additional 21 days.

- Pan forms may be removed after three days if pans are designed for early removal.  Soffit boards shall not be disturbed and shall not be removed for a minimum of eight days.

- Under ordinary weather conditions, wall forms, column forms, side of beam forms and other vertical forms for concrete which do not span between definite supports may be removed after two days.

- Forms for footings may be removed after 24 hours under ordinary weather conditions.

- When ambient air temperature falls below 45 degrees F during the curing period form removal shall take place based on job-cured test cylinder strength only.

- After removing forms, horizontal members shall be promptly re-shored at mid-span until the 28-day strength of concrete is attained.  No floor shall be loaded in excess of live load for which designed unless adequate shores are placed beneath members supporting the concentration of load.

- Under no circumstances shall wood be buried in full or left in contact with earth. All wood formwork shall be removed unless noted or specified otherwise.

- Care shall be taken in the removal of the forms to avoid damage to concrete surfaces.  Immediately after the forms are removed, all damaged or imperfect work shall be patched, or, if the work is severely damaged or unacceptable, it shall be rebuilt.  Remove all fins from exposed concrete surfaces immediately on removal of forms.

- Forms to be reused shall be thoroughly cleaned and repaired.  Split, frayed, delaminated, or otherwise damaged forms shall not be used.

- REINFORCING STEEL

- Shop fabricate from approved shop drawings.  Bars shall not be heated for bending.  Return all horizontal bars 2'-0" (or provide individual corner bars) at all corners and intersections in all concrete walls and footings.  All bars marked continuous shall be lapped with a Class "B" tension splice, including at corners. Splices shall be located as shown in accordance with CRSI Standards.  Provide diagonal corner bars at corners of all openings in slabs and walls.  Use 2-#5 X 4'-0" each corner, each face. If embedment length is not available provide standard hook. General placement and bar coverage shall be in accordance with ACI 318.

- At job site store at least 12" above ground.  Bars shall be free of foreign matter.  A thin coating of orange rust resulting from short exposure will not be considered objectionable.

- Reinforcement which has been exposed for bonding with future work shall be protected from corrosion by heavy wrappings of burlap saturated with a bituminous material.

- Notify the Engineer at least 24 hours prior to scheduled pouring of concrete for inspection of reinforcing steel.  No concrete shall be poured until reinforcement placement is approved.  Such approval shall not relieve the Contractor of his responsibility for correctness and compliance with the Contract Documents.

- PRODUCTION OF CONCRETE

- Concrete shall be produced in an approved central mixing plant in accordance with ASTM C-94.

- Unless otherwise called for on the drawings, concrete shall develop a compressive strength at 28 days, when tested in accordance with the applicable sections of ASTM, as follows:

- Interior floor slabs and footings - 3000 psi

- Columns, beams, walks, curbs and concrete exposed to the weather - 4000 psi.

- PLACING OF CONCRETE

- Concrete shall be placed in compliance with the applicable sections of the ACI.  Special attention shall be given to the requirements for slump, testing, curing, tolerances and placing during severe weather.

- Forms shall be free of ice, water, hardened concrete, and debris and items to be embedded shall be in position.

- Subgrades shall be sprinkled sufficiently to eliminate water loss from concrete.  Concrete shall not be placed on frozen ground.

- Concrete shall be transported by methods to avoid segregation.  Do not use vibrators to transport concrete in forms.  Concrete shall be placed rapidly and continuously and as close to its final position as possible. If construction joints are required they shall be placed at a location causing the least effect on the structural integrity of the work.

- Concrete shall be consolidated by vibration, spading and rodding.  Work concrete around reinforcement and embedded items.

- Provide a drainage system for all retaining walls that are a part of the structure.

- Coordinate all drawings for proper slope of floor to drains in toilets, showers and similar areas.

- TESTING

- The verification and control of concrete mixes shall be the work of an independent testing laboratory.  The selection of laboratory and cost of testing shall be paid for by the Owner unless other arrangements are made.

- LABORATORY SERVICES

- Test aggregates, cement and water for specification compliance.  During construction, the Engineer may require field inspection, sampling, and testing of cement, aggregates, etc. testing laboratory in order to determine if the requirements of this specification section are being satisfied.

- Prepare trial mix for each class of concrete, make and break test cylinders.  A minimum of two cylinders shall be tested at 7-days and 28-days.

- Make slump test and air content test at job site for each sample tested for compressive strength.

- Test cylinders shall be made and tested as follows:

One (1) set of five (5) cylinders shall be made for each fifty (50) cubic yards or fraction thereof for each class of concrete in each day’s pour.  Of each set of test cylinders, two (2) shall be broken at seven (7) days, two (2) shall be broken at 28-days, and one (1) held in reserve.

Test cylinders will normally be laboratory-cured.  However, the Engineer may require tests on field-cured specimens to check the adequacy of curing operations.

- Reports on all tests conducted by the laboratory shall be rendered promptly and distributed as follows:

Architect                	 One - (1) copy

Contractor                	 Two - (2) copies

Structural Engineer 	 One - (1) copy

Report of control cylinders for job placed concrete shall contain the following:

- Time of batching

- Time of sampling

- Concrete and air temperatures

- Slump

- Other information furnished by the General Contractor

- CONTRACTORS FUNCTION

- Contractor shall advise testing agency in advance of operations to allow for assignment of testing personnel and shall provide reasonable labor and assistance in obtaining, handling and storing test samples at the site.

- Contractor shall observe procedures of laboratory personnel molding and handling test specimens and if he observes any irregularities of procedures, he shall report them in writing to the Architect within 48-hours.

- Contractor shall keep a daily log recording quantities of each class of concrete used, the area location of each quantity of concrete relating to its controlling cylinder and the slump of this concrete, and general weather conditions.  The contractor shall furnish this information to the laboratory for inclusion in the test report. The Contractor shall obtain delivery tickets showing the class and strength of concrete, the size of coarse aggregate and the slump order.  The Contractor shall identify these tickets relative to the area of placement of the concrete and shall retain them on file. He shall produce the tickets should the Architect/Engineer so request.

- PRECAUTIONS

- Styrofoam shall not be used as joint filler.

- Manufactured sand shall not be used for fine aggregate.

- Severe weather concreting shall be in accordance with ACI-305 and ACI-306.

- Retempered concrete shall not be used.

- Defective Work - No materials or concrete which fail to conform to the requirements of this specification section shall be incorporated into the work.

- Water stops shall be continuous.  Do not use lap joints.

- The placing of dowels after concrete is poured is prohibited.  Bars partially embedded in concrete shall not be field-bent.

- Calcium chloride shall not be used.

- CLEAN-UP

- After completion of work, remove from the site all excess materials and debris.

END OF SECTION