PART I - GENERAL

1.01	DESCRIPTION

- The work covered by this Section consists of furnishing all labor, equipment, and material required for the correct placement and construction of concrete masonry units and related work as described herein and/or shown on the Drawings.

- Work for Other Trades: Bolts, anchors, and shelf angles shall be the responsibility of the Contractor.  However, the subcontractors requiring such work are responsible for furnishing complete information to the Contractor.

1.02	SUBMITTALS

- Samples:  Submit two full-size concrete masonry units of each type, including special shapes required to show range of colors, texture, finishes, and dimensions.

- Certificate:  Furnish manufacturer's written certification accompanied by suitable laboratory or mill test reports that masonry units furnished meet or exceed the requirements of this specification.

1.03	PRODUCT DELIVERY, STORAGE AND HANDLING

Store masonry units above ground on level platforms, which allow air circulation under stacked units.  Cover and protect against wetting prior to use.  Handle units on pallets or flat bed barrows.  Do not permit free discharge from conveyor units or transporting in mortar trays.

PART II - PRODUCTS

2.01	MATERIALS

- Concrete Masonry Unit: Hollow bearing units shall conform to ASTM C 90, Grade N, Type I, normal weight.  Nominal face dimension shall be 8 by 16 inches, except where otherwise noted on the Drawings.  All masonry units shall be obtained from a single manufacturer whose manufacturing and curing facilities are acceptable to the Engineer.

- Reinforcement:  Block wall reinforcement shall be of the prefabricated type for use in masonry mortar joints.  Wall reinforcement shall be of truss design for composite wall construction with No. 9 gauge deformed galvanized side be placed in first and second bed joint above and below openings, as specified above, and in every second bed joint throughout the remainder of the wall.

- Reinforcement in the first bed joint immediately above and below openings shall be continuous.  In the second bed joint it shall extend 2 feet beyond each side of the opening.  Reinforcing shall be lapped a minimum of 6 inches at splices.  Corner and abutting wall reinforcement shall be prefabricated corner and tee sections.

- Precast Sills and Lintels: Precast concrete sills, coping, trim, and lintels shall be provided as shown on the Drawings.  All exterior sills, coping, and trim shall be constructed of white portland cement and light granite aggregate.  Interior lintels shall be constructed of gray portland cement and marble aggregate.  All exposed surfaces shall be ground and treated with a water-repellent material.

- Contractor shall submit detail drawings of precast sills, coping, and lintels for approval by the Engineer before proceeding with fabrication.  Finished precast units shall be thoroughly protected against chipping and in no case will chipped surfaces or corners be permitted to remain in walls or copings.

PART III - EXECUTION

3.01	ERECTION AND WORKMANSHIP

- Scaffolding shall not be overloaded and shall be inspected regularly by the Contractor to see if it is amply strong, well braced, and securely positioned.  The Contractor shall be unconditionally responsible for the safety of the scaffolding at all times.

- Masonry shall not be laid when the temperature is below 40 degree F.  Walls shall be carried up level and plumb all around.  Unfinished work shall be stepped face for joining with new work; toothing shall not be permitted.  Heights of masonry shall be checked by the Contractor with an instrument at each floor and at sills and heads of openings to maintain the level of the walls.

- Masonry units shall be handled with care to avoid chipping, cracking, and spalling of faces and edges.  Drilling, cutting, fitting, and patching to accommodate the work of others shall be performed by qualified masons.  Masonry shall be cut with a masonry saw outside buildings.  Chipping or breaking with a hammer will not be permitted.

- Door and window openings, louvered openings, anchors pipes, ducts, and conduits shall be built in carefully as the work progresses.  Ties and anchors shall be placed accurately.  Metal work specified elsewhere shall be placed in position as the work progresses.  Grouting of ties and anchors into hardened mortar or grout shall not be permitted.

- Masonry units shall be laid in running bond.  The first course of masonry shall be laid in a full bed of mortar; and the succeeding courses shall be shoved (not laid) in beds of mortar to fill the joints full without subsequent flushing and filling.  Unless shown or specified otherwise, all joints shall be 3/8-inch thick.  Where ties, anchors and bolts occur within the cells of the units, such cells shall be filled with mortar or grout as the work progresses.

- Concrete masonry units shall be dry when laid.  Each unit shall be adjusted to final position in the wall while the mortar is still soft and plastic.  Any unit disturbed after mortar has stiffened shall be removed and relaid with fresh mortar.  Vertical cells to be filled with grout shall be aligned to provide a continuous unobstructed opening of the dimensions shown.  Chases shall be plumb and shall be minimum one-unit length from jambs of opening.

- Masonry joint reinforcement shall be placed so that longitudinal wires are located over face wall mortar beds and are fully embedded in mortar for their entire length with minimum mortar cover of 5/8 inch on exterior side of walls and 1/2 inch at other locations.

- Joints shall be finished with smooth concave contour.  Procedure used in striking joints shall be as follows: First strike the bed joints; next strike the head joints; then strike bed joints as required to remove any spots, etc., from intersection of bed and head joints.  After mortar has initial set but before mortar is hard, restrike the head joints to provide clean, smooth intersection of the head and bed joints.

- At the end of each day's work, the tops of exposed masonry walls shall be covered with a strong, nonstaining waterproof membrane well secured in place.  Surfaces not being worked on shall be properly protected at all times.  Unfinished work shall be stepped for joining with new work.  Before new work is started, all loose mortar shall be removed and the exposed joint thoroughly wetted, not less than 1/2 hour before laying new work.

- All cavities in exterior masonry walls shall be filled with loose fill insulation in accordance with the requirements of the section entitled "Building Insulation" of these Specifications.

3.02	CLEANING

- During construction, care shall be taken to keep exposed face of masonry clean of mortar and other stains.  Joints shall be raked as they reach thumbprint hardness. The exposed work shall then be brushed with a soft fiber brush to remove adhering mortar.  A wooden paddle shall be used to remove more tenacious material.  Bases of walls shall be protected from splash stains by covering the adjacent floor or ground with sand, sawdust, or polyethylene film.

- At completion of work, holes in exposed masonry shall be pointed and defective joints shall be cut out and tuck pointed solidly with mortar.

- If necessary, exposed masonry surfaces shall be scrubbed with warm water and soap and fiber brush and thoroughly rinsed with clear water.  Work that may be damaged, discolored, or stained shall be protected during the cleaning process.  The use of sapolio or wire brushes or acid for washing down walls shall not be permitted.

- Protect all finished work against freezing for a period of not less than 48 hours by means of enclosures, temporary heat, or such other protective methods as may be required and directed by the Engineer.

END OF SECTION